مشخصات فنی نوار تفلون
TEFLON TAPE                                                 
 THREAD SEAL P.T.F.E (TEFLON) TAPE                           
 ACC. TO BS 4375/68 TO BE  USED FOR LIQUID                   
 AND NATURAL GAS STEAM AND WATER CONNECTIONS                 
 SUPPLIER: "TEFLON ZANJAN" OR "MISHAB" OR "TEFLON TEHRAN" OR 
 "PIPEPAC PTFE"OR"T.B.A" OR "JOHN CRANE"OR"JOHNS MANVILLE"   
 LOCATION: ALL AREAS AND SOUTH PARS                          
 NOTE: FOR USE ON FUEL LINE, CONNECTION OF                   
 ALL ENGINE AND EQUIPMENT.                                   
 THICK. 0.075 MM.
WIDTH 12 MM.                     
